## Slide 1
Results of R&T CNES project
Evaluation of reliability of DSM technologies
Impact of aging on EMC of integrated circuits
Alexandre BOYER
Alexandre.boyer@insa-toulouse.fr
Notes: <number>

## Slide 2
Summary
Context and Problematic
EMR Characterization
Impact of Aging on IC Emission / Susceptiibility
On the EMR Prediction
Conclusion and Perspectives

## Slide 3
Electromagnetic emission
Intersystem Interferences
Intrasystem Interferences
Component
Susceptibility to EMI
Equipments
Board
Radar
Failure
Context - EMC of ICs
EMC requirements at IC level to ensure system EMC compliance

## Slide 4
Context – Aging of electronic systems
Overvoltage, EOS
Harsh conditions (T°c, moisture, vibration…)
Impact of IC aging ?
Emission level
f
dBµV
EMC tests
Compliance checking
Susceptibility level
f
dBm
Electromagnetic Reliability
EMC compliance can be affected !

## Slide 5
Problematic in R&T CNES project
Does circuit aging have a significant impact on EMC of Deep Submicron Integrated Circuit ? On Emission ? On Susceptibility ?
How can we accurately characterize the impact of aging on Integrated Circuit EMC ?
Can we predict the impact of circuit aging on Emission and Susceptibility level ?
Can we predict the impact of IC emission / susceptibility level drift on system safety ?

## Slide 6
Electromagnetic Reliability characterization
Number of sample (significant level of confidence)
EMC tests (depending on the mission profile)
Aging stress (depending on the mission profile)
Tests set-up optimization (Time, cost, accuracy)
Experimental set up
EMC level measurements
Accelerated aging (temperature, voltage stress)
Measurement error budget
Maximum EMC level drifts
Average EMC level drifts
EMC level dispersion drift
Data processing
Statistical analysis
Outputs
EMC failure rate (risk of non compliance for the full lifetime)
Readjustment of EMC margin (to compensate aging effects)
Still operating ?

## Slide 7
Impact of Aging on IC Emission
Case study 1
Significant … but small variations of emission level.
High temperature and thermal cycling combined to electrical stress reduces emission level
Electrical overstresses increase emission level.
A. Boyer, A. C. Ndoye, S. Ben Dhia, L. Guillot, B. Vrignon, “Characterization of the Evolution of IC Emissions after Accelerated Aging”, IEEE Transactions on EMC, Vol. 51, N°4, November 2009, pp 892 – 900
Conducted emission on power IC circuit (CMOS 0.35 µm).
Various type of stress (High T°c, thermal cycling, ESD, EOS)

## Slide 8
Case study 2
Measurement of simultaneous switching noise from digital I/O (CMOS 65 nm ST-LP).
High and Low temperature Operating Life tests.
S. Ben Dhia, A. Boyer, B. Li, A. C. Noye, “Characterization of the Electromagnetic behavior drifts of a nanoscale IC after Accelerated Life Tests”, Electronic Letters, 18th February 2010, Vol. 46, no. 4.
Average drift = - 0.7 dB
Average reduction of emission level.
Impact of Aging on IC Emission

## Slide 9
Impact of Aging on IC susceptibility
Case study 3
Conducted susceptibility tests on various digital and analog blocks designed in CMOS 0.25 µm
A. Boyer, B. Li, S. Ben Dhia, C. Lemoine, “Impact of aging on the immunity of a Mixed-signal circuit”, EMC Europe 2010, September 2010, Wroclaw, Poland.
 | Mean drift (dB) | Dispersion (dB)
Core0 | 0.1 | 1.35
Core1 | -0.35 | 1.45
Core2 | 0.49 | 2.04
IO | 0.51 | 1.21
PLL – Phase comparator | -1.06 | 2.22
PLL - VCO | -2.57 | 3.64

## Slide 10
Impact of Aging on IC EMC ?
Emission levels are slightly reduced after circuit aging.
However immunity to interferences can be strongly affected.
Influence on component dispersion in term of EMC levels.
Dependence with the technology ? Difficult to answer
Larger dependence with circuit function and design.
Why circuit can become more sensitive to voltage fluctuations ?
How can we predict immunity level drift induced by integrated circuit aging ?

## Slide 11
 | Origins | Effects at device level
EM | High current density | Interconnect resistance increase
HCI | High drain voltage, low T°c | Mobility Uo decrease Threshold voltage Vth increase
NBTI | Negative bias on gate, high T°c | Mobility Uo decrease Threshold voltage Vth increase
TDDB | High gate voltage, high T°c | Mobility Uo decrease Threshold voltage Vth increase
Before aging
After aging
Impact on circuit performances
On the EMR Prediction
Degradation mechanisms at transistor level

## Slide 12
On the EMR Prediction
Degradation mechanisms at transistor level
Example of characterization of device degradation mechanisms.
Technology Freescale CMOS 90 nm.
Extraction of transistor parameter variation laws.
Isat decrease
Vth increase

## Slide 13
On the EMR Prediction
IC immunity model: ICIM formalism (IEC 62433-4)
Characterize device degradation and include « aged » device model in susceptibility model
EMI
Integrated Circuit
Failure
Integrated Circuit Immunity Model

## Slide 14
On the EMR Prediction
Simulation flow for prediction of immunity level drift
Library of “fresh” devices
Library of “aged” devices
Device characterization (HCI, NBTI, TDDB stress)
Functional analysis before aging
Functional analysis after aging
Failure analysis (location, failure model)
PDN modeling
ICIM before aging
ICIM after aging
Prediction of immunity level before/after aging

## Slide 15
Case study 4
On the EMR Prediction
Immunity modeling of a 0.25 µm CMOS PLL
Include impact of accelerated aging (high temperature operating life test)
Degradation of voltage-controlled oscillator characteristics which alters its immunity to power supply voltage fluctuations
Measurement (worst case sample)
Simulation
Max drift = -6 dB
Average drift = -1.6 dB
B. Li, A. Boyer, S. Ben Dhia, C. Lemoine, “Ageing effect on electromagnetic susceptibility of a phase locked loop”, Microelectronics Reliability, Vol. 50, Issues 9-11, September – November 2010, pp. 1304-1308.
Max drift = -10 dB
Average drift = -2.6 dB

## Slide 16
Conclusion / Perspectives
Different case studies studied in R&T CNES project have shown that aging can alter emission and susceptibility levels of integrated circuits.
Combined to long-term reliability issue in DSM technology, ensuring long-term EMC compliance becomes a challenge.
A major issue concerns the prediction of EMC level drift.
A prediction methodology is proposed, based on degradation mechanism characterization.
Perspectives : Nanospace test chip
Characterization of degradation mechanisms
Measurement and modeling of emission/susceptibility drift induced by aging
Impact of aging on circuit PDN
Impact of aging on EMC oriented guidelines

## Slide 17
Publications
A. Boyer, A. C. Ndoye, S. Ben Dhia, L. Guillot, B. Vrignon, “Characterization of the Evolution of IC Emissions after Accelerated Aging”, IEEE Transactions on EMC, Vol. 51, N°4, November 2009, pp 892 – 900.
S. Ben Dhia, A. Boyer, B. Li, A. C. Noye, “Characterization of the Electromagnetic behavior drifts of a nanoscale IC after Accelerated Life Tests”, Electronic Letters, 18th February 2010, Vol. 46, no. 4.
B. Li, A. Boyer, S. Ben Dhia, C. Lemoine, “Ageing effect on electromagnetic susceptibility of a phase locked loop”, Microelectronics Reliability, Vol. 50, Issues 9-11, September – November 2010, pp. 1304-1308.
B. Li, A. C. Ndoye, A. Boyer, S. Ben Dhia, “Characterization of the electromagnetic robustness of a nanoscale CMOS integrated circuit”, EMC Compo 2009, Toulouse, November 17 – 19 2009
A. Boyer, B. Li, S. Ben Dhia, C. Lemoine, “ Impact of Aging on the Immunity of a Mixed Signal Circuit”, EMC Europe 2010, 13 – 17th September 2010, Poland
E. Sicard, A. Boyer "IC-EMC v1.5 User's Manual", INSA editor, pp. 80 - 112, ISBN 978-2-87649-052-9, online at www.ic-emc.org